**System: A-Turf® Premier RSM**

|  |  |
| --- | --- |
| Face Yarn Type: | 100% polyethylene parallel-long slit fiber (TenCate XP Blade or XP Blade + \*\*\*other fiber brands available) |
| Yarn Size:  | 8,000 (single end per needle) or 10,000 denier |
| Yarn Thickness:  | 100 microns |
| Pile Weight:  | 40 oz/sy typical |
| Finished Pile Height:  | 2.5"  |
| Field Color: | Field Green, or Field Green/Lime Green, |
| Construction:Stitch Rate:Gauge: | Broadloom tufted, 8/3" +/-3/8” |
| Primary Backing:  | TenCate XK TuffBack |
| Secondary Backing: | 20 oz/sy urethane typical |
| Total Carpet Weight:  | 68 oz/sy (+/- 2 oz) typical |
| Turf Roll Dimensions:  | 15' wide by custom lengths up to 220' |
| Perforations:  | 3/16" holes on staggered 4" (approximate) centers |
| Turf Permeability:  | > 40" +/- per hour |
| Infill Composition: | 3 lbs of rubber, 6lbs of sand per square foot |
| Field Markings:Total System Weight: | Tufted, inlaid, or painted1,364 oz/sy |
|  |  |
|  |  |

*Specifications are subject to change without notice.*