**System: A-Turf® Mono-RSM**

|  |  |
| --- | --- |
| Face Yarn Type:  | 100% polyethylene monofilament fiber (TenCate Monoslide Ultra XQ \*\*\*other fiber brands availble)  |
| Yarn Size:  | 10,800 denier (6 ends/1,800 denier per end) |
| Yarn Thickness:  | 310 microns ( for Monoslide Ultra XQ) |
| Pile Weight: | 45 oz/sy |
| Finished Pile Height:  | 2.5” |
| Field Color:  | Field Green, Field Green/Lime Green,  |
| Construction:Stitch Rate:Gauge:  | Broadloom tufted8/3” +/-½”  |
| Primary Backing: | TenCate XK TuffBack |
| Secondary Backing: | 22 oz/sy urethane typical  |
| Total Product Weight:  | 73 oz/sy (+/- 2 oz) typical |
| Turf Roll Dimensions:  | 15' wide by custom lengths up to 220' |
| Perforations:  | 3/16" holes on staggered 4" (approximate) centers |
| Turf Permeability:  | > 40" +/- per hour |
| Infill Composition:  | 3 lbs rubber and 6 lbs sand per square foot. |
| Field Markings:  | Tufted, inlaid, painted  |
| Total System Weight: | 1,371 oz/sy |

*Specifications are subject to change without notice.*