**System: A-Turf® Premier RSM**

|  |  |
| --- | --- |
| Face Yarn Type: | 100% polyethylene parallel-long slit fiber (TenCate XP Blade or XP Blade + \*\*\*other fiber brands available) |
| Yarn Size: | 8,000 (single end per needle) or 10,000 denier |
| Yarn Thickness: | 100 microns |
| Pile Weight: | 40 oz/sy typical |
| Finished Pile Height: | 2.5" |
| Field Color: | Field Green, or Field Green/Lime Green, |
| Construction:  Stitch Rate:  Gauge: | Broadloom tufted,  8/3" +/-  3/8” |
| Primary Backing: | TenCate XK TuffBack |
| Secondary Backing: | 20 oz/sy urethane typical |
| Total Carpet Weight: | 68 oz/sy (+/- 2 oz) typical |
| Turf Roll Dimensions: | 15' wide by custom lengths up to 220' |
| Perforations: | 3/16" holes on staggered 4" (approximate) centers |
| Turf Permeability: | > 40" +/- per hour |
| Infill Composition: | 3 lbs of rubber, 6lbs of sand per square foot |
| Field Markings:  Total System Weight: | Tufted, inlaid, or painted  1,364 oz/sy |
|  |  |
|  |  |

*Specifications are subject to change without notice.*