**System: A-Turf® Titan RSM**

|  |  |
| --- | --- |
| Face Yarn Type:  | Polyethylene TenCate XP Blade and Monoslide Ultra XQ blended in dual yarn types and dual yarn thicknesses |
| Yarn Size:  | 12,200 (4 ends/1,800 denier per end for Mono, 5,000 denier per end for XP) |
| Yarn Thickness:  | 100 microns for XP Blade, 310 microns for Monoslide Ultra XQ  |
| Pile Weight:  | 45 oz/sy  |
| Finished Pile Height:  | 2.5"  |
| Field Color:  | Field Green, Field Green/Lime Green (dual colors as alternating panels or blended fibers)  |
| Construction:Stich Rate:Gauge: | Broadloom tufted8/3 +/-1/2"  |
| Primary Backing:  | TenCate XK TuffBack  |
| Secondary Backing:  | 22 oz/sy urethane typical (required for 12-year warranty)  |
| Total Carpet Weight:  | 75 oz/sy (+/- 2 oz)  |
| Turf Roll Dimensions:  | 15' wide by custom lengths up to 220' |
| Perforations:  | 3/16" holes on staggered 4" (approximate) centers |
| Turf Permeability:  | > 40" +/- per hour |
| Infill Composition:  | 3 lbs rubber and 6 lbs sand per square foot. |
| Field Markings:  | Tufted, inlaid, painted  |
| Total System Weight:  | 1,371 oz/sy \*Includes infill. |

*Specifications are subject to change without notice.*