**System: A-Turf® Titan RSM**

|  |  |
| --- | --- |
| Face Yarn Type: | Polyethylene TenCate XP Blade and Monoslide Ultra XQ blended in dual yarn types and dual yarn thicknesses |
| Yarn Size: | 12,200 (4 ends/1,800 denier per end for Mono, 5,000 denier per end for XP) |
| Yarn Thickness: | 100 microns for XP Blade, 310 microns for Monoslide Ultra XQ |
| Pile Weight: | 45 oz/sy |
| Finished Pile Height: | 2.5" |
| Field Color: | Field Green, Field Green/Lime Green (dual colors as alternating panels or blended fibers) |
| Construction:  Stich Rate:  Gauge: | Broadloom tufted  8/3 +/-  1/2" |
| Primary Backing: | TenCate XK TuffBack |
| Secondary Backing: | 22 oz/sy urethane typical (required for 12-year warranty) |
| Total Carpet Weight: | 75 oz/sy (+/- 2 oz) |
| Turf Roll Dimensions: | 15' wide by custom lengths up to 220' |
| Perforations: | 3/16" holes on staggered 4" (approximate) centers |
| Turf Permeability: | > 40" +/- per hour |
| Infill Composition: | 3 lbs rubber and 6 lbs sand per square foot. |
| Field Markings: | Tufted, inlaid, painted |
| Total System Weight: | 1,371 oz/sy \*Includes infill. |

*Specifications are subject to change without notice.*